## Slide 1
Weekly checkin on March 9th
WSe2 FETs ambipolarity question
NPG Asia Mater 10, 703–712 (2018).
Siyuan’s device (3L)
My device
Other studies suggest monolayer WSe2 device doesn’t easily show ambipolar curve
Potential question mark on anything thicker than bilayer
Still, monolayer device looks deeply OFF with both Au and Pd contact

## Slide 2
Weekly checkin on March 9th
ALD HfO2 thermal conductivity question
It seems like WSe2 are all burned after spectroscopic mapping @ 0.6 mW for 5 s
ALD HfO2 reportedly has worse heat conductivity than ALD Al2O3
Potential problem for further optical measurements?